| Tag No. «Name» - «Description» |  |  |  |
| --- | --- | --- | --- |
| Subsystem: «ProcessBreakdownIdentifier» - «ProcessBreakdownName» |  |  |  |
| Drawing No. | «DocumentList» | Task No. | «TaskName» |
| Additional Information: | «Comments» |  |  |

| ITP Ref / No.: |  |
| --- | --- |
| Location / Area / Lot |  |

| Item No | Description | Completed by |  | Accepted by |  | Comment |
| --- | --- | --- | --- | --- | --- | --- |
| ITEMS TO BE CHECKED PRIOR TO APPROVAL |  | Initials | Date | Initials | Date |  |
|  | Approve previous layer accepted and Survey Data Report provided: - Embankment foundation approved by the Client, refer to C1.010 or - Embankment Construction Last layer approved by the Client, ref C1.011 |  |  |  |  |  |
|  | Define lots and set out works: - Place survey pegs to an offset the height of the embankment lift to ensure correct compaction |  |  |  |  |  |
|  | Prior to Placement Capping - Borrow pit management plan in place and approved, excavation permit in place - Datum agreed with the Client - Does previous layer sufficiently conditioned |  |  |  |  |  |
| Hold Point | Have items 1-3 been checked |  |  |  |  |  |
|  | Material and Compaction Conformance - Conformed to Select Fill PSD grading - Liquid Limit ,<= 35% - Plasticity Index PI 4% – 17% - Linear Shrinkage <= 10% - CBR (4 day soaked) >= 60% - Compaction 150mm below surface level 98% MMDD and - Optimum Moisture Content ±2% OMC |  |  |  |  |  |
|  | Trim batter as per drawings and specification: - Trim both sides of batter to the design line - Clear all loose material from embankment, slope as per drawing |  |  |  |  |  |
|  | Complete As Built survey and check conformance - Bulk earthworks level tolerance is ±100mm - Finished earthworks level tolerance is +10/-25mm - Pavement deviation from design level ± 6mm - Deviation from a 3 m straight edge laid along the finished surface < 10mm - Deviation from batter line at any point along the batter <150mm (Survey every 20m each side of batter per Lot Length) - Surface Levels Survey – 3 points equally spaced apart per 10m strip (at the two edges and one in the middle) every 20m |  |  |  |  |  |
| Hold Point | Approval of final trim, layer placement and construction tolerances. |  |  |  |  |  |

| COMMENTS, OBSERVATIONS & ATTACHMENTS (NO PUNCHLIST ITEMS TO BE INCLUDED HERE) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| COMPLETED |  |  |  |  |  |
| I hereby confirm the work has been completed in accordance with Contract specified drawings, specifications & standards. |  |  |  |  |  |
| PERFORMED BY CONTRACTOR: |  | REVIEW BY SUPERVISOR/LEAD ENGINEER: |  | EPCM ACCEPTED BY: |  |
| Signature: |  | Signature: |  | Signature: |  |
| Name: |  | Name: |  | Name: |  |
| Title: |  | Title: |  | Title: |  |
| Date: |  | Date: |  | Date: |  |