| Tag No. «Name» - «Description» |  |  |  |
| --- | --- | --- | --- |
| Subsystem: «ProcessBreakdownIdentifier» - «ProcessBreakdownName» |  |  |  |
| Drawing No. | «DocumentList» | Task No. | «TaskName» |
| Additional Information: | «Comments» |  |  |

| ITP Ref / No.: |  |
| --- | --- |
| Location / Area / Lot |  |

| Item No | Description | Completed by |  | Accepted by |  | Comment |
| --- | --- | --- | --- | --- | --- | --- |
| ITEMS TO BE CHECKED PRIOR TO APPROVAL |  | Initials | Date | Initials | Date |  |
|  | Verify Lot for works has been identified, pegged and marked out (Survey Data Report) |  |  |  |  |  |
|  | Underlying Lot conforms - Ensure underlying lots conforms, all outstanding Items are closed and signed off - Underlying lot in acceptable state to start work, Ref. C1.011 or C1.012 |  |  |  |  |  |
|  | Verify Material Compliance Tests for Wearing Course: Test Frequency; - PSD, LL, PL, PI and Linear Shrinkage (1 test per 2500m³) - CBR Strength (1 test per 5000m³) Test Property: - LL 35% maximum - CBR (4 dry soaked) 60% minimum - PI 4-15% maximum - Gradient Coefficient 14-30 and - Shrinkage Product 140-400 |  |  |  |  |  |
| Hold Point | Have items 1-3 been checked |  |  |  |  |  |
|  | Construction of Wearing Course Place and Compact in layers (minimum): - 100mm for LME access roads and - 150mm for HME access roads. - Compacted thickness to level as specified in drawings. |  |  |  |  |  |
|  | Test Compaction of Placed Material - Field Density Test ≥98% MMDD, OMC ±2% - (Frequency: 1 test per layer or 300mm) - Thickness, per material type per 500m², or 1 test per 100m³ distributed reasonably evenly throughout full depth and area of layer; or 3 tests per visit per layer; whichever requires the most tests. |  |  |  |  |  |
|  | Surface Finish: - Rolling and trimming to final levels of the wearing course layer shall be completed whilst the surface is near optimum moisture and in a pliable condition. - The finished surface shall be of a homogeneous, uniformly bound condition with no evidence of layering or disintegration or lamination - The completed wearing course surface shall be maintained in a conforming condition to the specified tolerances, watered as necessary to prevent shrinkage cracking, dusting or loosening of its surface until formally handed over to the Engineer - Visual inspection of Completed Wearing Course layer to ensure that Work-lot area is free of any non-conforming items/ conditions. |  |  |  |  |  |
|  | Survey Wearing Course layer Width tolerance: - Deviation of batter line from the design batter at any point along the batter < 150mm - Surface level: ±6 mm - Survey Frequency – 3 points equally spaced apart per 10m strip (at the two edges and one in the middle) every 20m - As built, Survey Data Report (ASCON) Completed by Qualified surveyor Straight Edge Conformance: - Maximum of 10mm along a 3m straight edge. |  |  |  |  |  |

| COMMENTS, OBSERVATIONS & ATTACHMENTS (NO PUNCHLIST ITEMS TO BE INCLUDED HERE) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| COMPLETED |  |  |  |  |  |
| I hereby confirm the work has been completed in accordance with Contract specified drawings, specifications & standards. |  |  |  |  |  |
| PERFORMED BY CONTRACTOR: |  | REVIEW BY SUPERVISOR/LEAD ENGINEER: |  | EPCM ACCEPTED BY: |  |
| Signature: |  | Signature: |  | Signature: |  |
| Name: |  | Name: |  | Name: |  |
| Title: |  | Title: |  | Title: |  |
| Date: |  | Date: |  | Date: |  |